Component				Formula	Typical %		Specification

Min	Max

Magnesium Chloride			MgC12		33.3			31	35

Potassium Chloride			KC1		24.3			23	30

Sodium Chloride			NaC1		5.5			1.5	9

Calcium Chloride			CaC12		0.2			0.06	0.5

Water					H2O		36.4			32	40

Sulphate				(SO4)		0.15			0.05	0.2

Bromide				Br-		0.5			0.3	0.6

Granular Size

Fine Grade:		Min 90% 		< 1.7mm

Coarse Grade:	Min 90%  		Between 1.7mm to 6.5mm

Available in 25 kg bags (42 or 49 per pallet)