Name, formula:		Sodium Chloride, NaCl

Trade name:			Marine Salt De Icing Grade

Typical chemical analysis:	NaCl			≥99.0%

Sulphate SO4		<0.5%

Insolubles		≤0.15%

H20			<3.5% (loss of mass at 110c)

Moisture		≤4% (loss of weight at 110c)

Typical screen analysis:	Above 8mm     	< 1%

Passing 6.3mm 	≤ 5%

Passing 0.315mm	 ≤ 5%

Treated with Anti-caking treatment 50 mg/kg

Forms of delivery:

Bulk:				By pneumatic tanker or tipper lorry

Bags:				1000kg bags

28 per lorry load

This specification is given as an indication.  Being a natural product, variations can occur.

This product complies to BS3247:2011