Name, formula:		Sodium Chloride, NaCl

Trade name:			Marine Salt De Icing Grade

Typical chemical analysis:	NaCl				≥99.0%

Sulphate SO4			<0.5%

Insolubles			≤0.15%

H20 				<3.5%	(loss of mass at 110c)

Moisture			≤4% (loss of weight at 110c)

Typical screen analysis:	Above 8mm    			 < 1%

Passing 6.3mm 		 ≤ 5%

Passing 0.315mm 		≤ 5%

Treated with Anti-caking treatment 50 mg/kg

Forms of delivery:

Bulk:				By pneumatic tanker or tipper lorry

Bags:				In 10kg polythene bags on pallets

120 x 10kgs = 1200kgs

This specification is given as an indication.  Being a natural product, variations can occur.

This product complies to BS3247.