Chemical Analysis		Typical Value

Moisture			max 0.06 %		as H2O

Calcium			max 0.15 %		as Ca

Magnesium			max 0.05 %		as Mg

Insolubles in water		max 0.05 % 		Insolubles

Sulphate			max 0.02 %		SO4

Assay (dry basis)		98.5 – 99.5 %		as NaCl

Salt Tablet Dimensions

Diameter	25mm

Height		14 mm

Weight		11gr

Country of Origin

Turkey

HS Code No

25010051