# Chemical Analysis				Typical			Specification

# Min 	Max

NaC1 (calculated on dry basis)			99.8%			  99.5	99.9%

Ca						0.04%			  0.01	0.08%

Mg						0.03%			  0.01	0.05%

S04						0.12%			  0.04	0.25%

Insolubles					0.01%			  0	0.03%

H20						0.1%			  0.05	0.15%

Anti caking agent (E535)			15mg/kg max

Granular size

Minimum 80% passes through 0.71mm sieve opening (No.25)

Packing / Delivery format:

10kg bags – 120 per pallet

25kg bags – 49 per pallet

Shelf life

Within 5 years from the production date.

Storage Condition

Store in protected dry shadowed area

Country of Origin

Israel