Name, formula:		Sodium chloride & Peacock 563 Corrosion Inhibitor

Trade name:			Pro Brine

Appearance:	Liquid, odourless

Typical Analysis

| Sodium Chloride NaCl | 99.5% (Dry basis) |
| --- | --- |
| Calcium Sulphate Ca SO4 | 0.05% |
| Magnesium Sulphate Mg SO4 | 0.05% |
| Magnesium Chloride MgC1 | 0.01% |
| Peacock 563 Corrosion Inhibitor | 30% (Mixed Soln.) |
| Bulk density: | 1.05 - 1.25 g/cm3 According to DIN (ISO) 3944 |

Chemical Composition

| Parameter | Units | Specification |
| --- | --- | --- |
| Sodium Chloride | % m/m | 23 min |
| Water Insolubles | mg/l | 50 max |
| Iron | mg/l | 0.1 max |
| Copper | mg/l | 0.01 max |
| Arsenic | mg/l | 0.2 max |
| Lead | mg/l | 0.05 max |

Peacock 563 Corrosion Inhibitor

| Remains a mobile liquid, even at low temperatures | Contains no secondary amines | Nitrite & boron free |
| --- | --- | --- |
| Prevents the staining of aluminium | Does not dry to form sticky or gummy residues | Low foaming tendency |
| hard water compatible | All components are approved for incidental food contact | Contains no solvents |
| Peacock 563 is effective at preventing the following metals from corroding: Copper alloys, Cadmium, Brass, Cast Iron, Steel, Aluminium Alloys, Zinc, Solders. |

Forms of delivery:    1000ltr IBC / 4 x 5ltr Tubs / 15ltr Jerry Can