Chemical Analysis				Typical	Specification

Min   Max

NaCl (calculated on dry basis)		99.8%		99.5 - 99.9%

Ca						0.04%		0.01 - 0.08%

Mg						0.03%		0.01 - 0.05%

SO4						0.1%		0.04 - 0.25%

Insolubles					0.01%		0      - 0.03%

H2O						0.1%		0.05 - 0.15%

E535 - Anti caking agent Na4 Fe (CN)	15mg/kg

Granular Size

Min 80% passes through 0.59mm sieve opening net (No 30)

Packaging

25kg PE Bags – 49 per pallet

Shelf Life

Within 5 years from Production date.

Storage Conditions

Store in protected dry shadowed area

Country of Origin

Israel