Aquasol is the ideal compacted salt product for regeneration of domestic and smaller commercial water softeners. Aquasol is used and recommended by some of the UK’s leading manufacturers of water softeners.

- Manufactured from pure dried vacuum salt to ensure purity

- Rapidly dissolves to produce premium quality brine

- Packed in a choice of bag sizes to suit customer requirements

- Manufacturing process accredited ISO 9001:2008

## Chemical 		BS EN973:2009	Typical

Analysis		Standard		Specification

Moisture		0.6% max		0.05%			as H2O

Water Insoluble	0.05% max		0.02%

Arsenic		13 mg/kg max		<0.006 mg/kg		as As

Cadmium		1.3 mg/kg max	<0.007 mg/kg		as Cd

Lead			13 mg/kg 		<0.006 mg/kg		as Pb

Mercury		0.26 mg/kg max	<0.002 mg/kg		as Hg

Nickel			13 mg/kg max		<0.001 mg/kg		as Ni

Antimony		2.6 mg/kg max	<0.008 mg/kg		as Sb

Selenium		2.6 mg/kg max	<0.008 mg/kg		as Se

Assay (dry basis)	99.4% min		99.75%		as NaCl

Packaging

Aquasol salt tablets are available in both:-

10kg polythene bags

25kg polythene bags

Palletised product is stretch wrapped for added protection during transit.