Pure Dried Vacuum Salt is ideal for a wide range of applications including food, animal feed, water treatment and chemical manufacture.  The manufacturing plant is registered for food production, and food grade PDV certified to the BRC Global standard for food safety and feed grade PDV certificated to the Feed Materials Assurance Scheme, FEMAS.  Low sulphate, bromide and moisture levels contribute to the high chemical purity which is required for most industrial applications.  This purity is assured by a Quality Management System registered to ISO 9001 and a commitment to continuous improvement.

CHEMICAL SPECIFICATION

Test methods used are as given in BS998:1990 or equivalent, except appearance which is a visual assessment.

COMPONENT 			UNIT 			SPECIFICATION 		TYPICAL

ANALYSIS

Appearance 						White Crystalline

Assay (dry basis) 		%m/m NaCl 		99.9 min. 			99.9

Surface Moisture 		%m/m H2O 		0.05 max. 			0.01

Insoluble matter 		mg/kg 			<50 				<10

Alkalinity 			mg/kg Na2CO3		<150 				62

Sulphate			mg/kg Na2SO4		<500 				175

E535, Sodium

Hexacyanoferrate II		mg/kg Na4Fe(CN)6	14 max. 			8.1

Total Iron 			mg/kg Fe 		<5 				1.5

Total Calcium 			mg/kg Ca 		<20 				3.1

Total Magnesium 		mg/kg Mg 		<5 				0.7

Total Copper 			mg/kg Cu 		2 max. 				<0.1

Total Arsenic 			mg/kg As 		0.3 max. 			<0.01

Total Lead 			mg/kg Pb 		1 max. 				<0.1

Total Cadmium 			mg/kg Cd 		0.2 max. 			<0.01

Total Mercury 			mg/kg Hg 		0.05 max. 			<0.03

Total Nickel 			mg/kg Ni 		0.75 max. 			<0.05

Total Chromium 		mg/kg Cr 		0.75 max. 			<0.03

Total Selenium 			mg/kg Se 		2.6 max. 			<0.2

Total Antimony 			mg/kg Sb 		2.6 max. 			<0.2

Total Bromide 			mg/kg Br 		<120 				83

PHYSICAL CHARACTERISTICS

Typical Pouring Density 		1.25 - 1.30 g/cm3

Typical Sieve Analysis 		BS410 ref. 	% Through Sieve

16 (1000μm) 		99.9

22 (710μm) 		99.7

30 (500μm) 		92.6

52 (300μm) 		28

85 (180μm) 		  4.8

Country of Origin:		England

Signed:	STACEY KEATING – QUALITY COORDINATOR