# Chemical Analysis				Typical			Specification

# Min 	Max

NaC1 (calculated on dry basis)			99.8%			  99.5	99.9%

Ca						0.04%			  0.01	0.08%

Mg						0.03%			  0.01	0.05%

S04						0.12%			  0.04	0.25%

Insolubles					0.01%			  0	0.03%

H20						0.1%			  0.05	0.15%

** Due to there not being any anti caking agent in this product, it is possible that it may compact and become hard**

Granular size

Minimum 80% passes through 0.71mm sieve opening (No.25)

Packing / Delivery format:

10kg bags – 120 per pallet

25kg bags – 49 per pallet

Shelf life

Within 5 years from the production date.

Storage Condition

Store in protected dry shadowed area

Country of Origin

Israel

Please note that the manufacturer refers to this product on their Organic Trading Schedule as Seasun Fine Sea Salt.

Stacey Keating

Quality Coordinator