Product

Urea Technical Grade Treated

Spec No BENSP00014

Physical Properties				Unit				Specification

Appearance					Pure white free flowing prills treated with an anti-caking

Additive: free from harmful substances.

Chemical Composition

Nitrogen					% ww				Min 46

Biuret						% ww				Max 1.0

Moisture					% ww				Max 0.5

Buffer Value					% ww				1.0 – 4.0

pH (10% urea solution)				Max				10

Ammonia and Ammonium Salts			Ppm w/w			150

Particle size 1.0 – 4.0mm			%				90

Packaging									25kg bags/500kg 									FIBC’s/100kg FIBC’s on or								off pallets

Packaging

25kg bags x   (polythene sacks on pallets)