Appearance                    White Crystalline Powder

PROPERTIES	Specification		     Typical

Assay (KCl)	95.0% min	97.3%

Potassium Oxide Equiv. K2O	60.0% min	61.5%

Sodium Chloride NaCl	 4.0% max	 2.3%

Moisture	0.20% max	 0.10%

Anti-caking Agent  -  Sepiolite (Feed Grade)	 1.00%

Bulk density	1.05mt/m3

Angle of repose	320

TYPICAL MESH ANALYSIS

SIEVE SIZE (mm)                   TYPICAL %  RETAINED               % RANGE

+1.18 (1180 µm)		1			0 - 2

+0.85 (850 µm)		2			1 - 5

+0.60 (600 µm)		8			2 - 20

+0.42 (420 µm)		22			15 - 55

+0.21 (210 µm)		78 			70 - 85

+0.10 (100 µm)			98		95 – 99

TRACE ELEMENTS

ELEMENT	TYPICAL (ppm)    	TYPICAL VARIATION

Magnesium (Mg)	       124.00	    49 - 262

Calcium (Ca)	187.00	    80 - 303

Iron (Fe)	  40.00	      6 - 180

Aluminium (Al)	  11.37	      1 - 85

Cadmium (Cd)	  <0.010                    <0.010 -  0.117

Mercury (Hg)	  <0.001                    <0.001 – 0.014

Copper (Cu)	  <0.10	  <0.10   –   1.69

Nickel (Ni)	    2.64	          0.35  – 612.7

Zinc (Zn)	  <0.20	        <0.20 – 22.80

Chromium (Cr)	  <0.05                        <0.05 – 4.65

Lead (Pb)	    2.85	          <1.64 – 3.90

Arsenic (As)	    0.47                        <0.10 – 1.75

Vanadium (V)	  <0.20	      <0.20 – 0.70

Boron (B)	  19.30                                3 - 35

This product is a naturally occurring material and its content is therefore subject to variation.

N.B.     	This material is primarily designed for use in the agricultural/horticultural and oil drilling industries. The presence of  small particles is normal and

whilst the product is screened prior to packing to eliminated larger foreign

matter, users should satisfy themselves as to its suitability if used for other

purposes.

Genetically Modified/Allergy Status

‘Potassium Chloride Treated Soluble’ is a deep mined product and

therefore does not contain dioxins or genetically modified organisms and is

allergen free.

Shelf Life

If stored in dry conditions and original unopened packaging the shelf life should not

be less than 1 year.

Country of Origin                                            United Kingdom