DESCRIPTION

A blended mixture of Pure Dried Vacuum Salt 98% and Boric Acid 2%

CHEMICAL SPECIFICATION – PURE DRIED VACUUM SALT

Test methods used are as given in BS998:1990 or equivalent, except appearance which is a visual assessment.

COMPONENT 			UNIT 			SPECIFICATION 		TYPICAL

ANALYSIS

Appearance 						White Crystalline

Assay (dry basis) 			%m/m NaCl 		99.9 min. 			99.9

Surface Moisture 			%m/m H2O 		0.05 max. 			0.02

Insoluble matter 			mg/kg 			<50 				<10

Alkalinity 			mg/kg Na2CO3		<150 				67

Sulphate				mg/kg Na2SO4		<500 				181

E535, Sodium

Hexacyanoferrate II		mg/kg Na4Fe(CN)6	14 max. 				6.7

Total Iron 			mg/kg Fe 		<5 				1.3

Total Calcium 			mg/kg Ca 		<20 				2.4

Total Magnesium 		mg/kg Mg 		<5 				0.7

Total Copper 			mg/kg Cu 		2 max. 				<0.1

Total Arsenic 			mg/kg As 		0.3 max. 			<0.01

Total Lead 			mg/kg Pb 		1 max. 				<0.1

Total Cadmium 			mg/kg Cd 		0.2 max. 			<0.01

Total Mercury 			mg/kg Hg 		0.05 max. 			<0.03

Total Nickel 			mg/kg Ni 		0.75 max. 			<0.05

Total Chromium 			mg/kg Cr 		0.75 max. 			<0.03

Total Selenium 			mg/kg Se 		2.6 max. 			<0.2

Total Antimony 			mg/kg Sb 		2.6 max. 			<0.2

Total Bromide 			mg/kg Br 		<120 				80

PHYSICAL CHARACTERISTICS

Typical Pouring Density 		1.25 - 1.30 g/cm3

Typical Sieve Analysis 		BS410 ref. 	% Through Sieve

16 (1000μm) 		100

22 (710μm) 		99.9

30 (500μm) 		97.1

52 (300μm) 		39.5

85 (180μm) 		9.0

CHEMICAL SPECIFICATION BORIC ACID

Boric Acid (H3BO3) 	99.99 – 100.20 %

Boric Oxide (B2O3) 	56.29 – 56.41 %

Typical 	Maximum

Sulphate (SO4) 		0.005 % 	0.01 %

Chloride (Cl) 			0.005 % 	0.0075 %

Iron (Fe) 			0.00015 % 	0.0003 %

Granulometry:-

Retained %

A.S.T.M. Sieve No.: 		20 (850μm) 	1.5 % max

# Bulk Density:-

MT/m3

Typical range 					0.85 – 0.95

PACKAGING

Packed in 1000kg IBC