Properties of Winter Wizard Salt Sticks –

Application

For de-icing purposes

K3 Rock Salt   	CAS-No	: - 7647-14-5		EINECS-No: 231-598-3

Packaging

1.5kg – 12 sticks per box

Chemical analysis		Typical		Methods

Sodium Chloride		99%			ASTM 534-98

Calcium  			0.3%			ISO 2482

Magnesium			0.02%			ISO2482

Sulphate			0.7%			ISO 2480

H2O-insoluble			0.15%			ISO 2479

Iron				5mg/kg		EuSalt AS015

Copper			0.08 mg/kg		EuSalt AS015

Physical Properties

Bulk density:			1.050 - 1.250 kg/m3	EN1236

Anti Caking Agent

E535, calculated as K4[Fe(CN)6]

Andydr. And E500		10mg/kg			EuSalt AS004