Hydrosoft Granular salt is the ideal regenerant for water softeners.  The large crystalline beads are easily dispersed and rapidly dissolve.  The unique manufacturing process of achieves food-grade purity and absence of mushing problems.  Product quality is assured by a Quality management system registered to ISO 9001, a manufacturing process certificated to the BRC Global Standard for Food Safety and a commitment to continuous improvement.

Chemical Specification

Test methods used are given in BS998:1990 or equivalent, except appearance which is a visual assessment.

| Property | Unit | Specification | Typical Analysis |
| --- | --- | --- | --- |
| Appearance |  | White Crystalline |  |
| Assay (dry basis) | %m/m NaCl | ≥99.9 | >99.9 |
| Surface Moisture | %m/m H2O | <1.0 | 0.16 |
| Insoluble matter | Mg/kg | <50 | <10 |
| Alkalinity | Mg/kg NaCO3 | <100 | 60 |
| Sulphate | Mg/kg Na2 SO4 | <300 | 160 |
| E535, Sodium Hexacyanoferrate II | mg/kg Na4Fe(CN)6 | 14 max | 6.5 |
| Total Iron | Mg/kg Fe | <5 | 1.4 |
| Total Calcium | Mg/kg Ca | <5 | 0.7 |
| Total Magnesium | Mg/kg Mg | <2 | 0.9 |
| Total Copper | Mg/kg Cu | 2 max | <0.1 |
| Total Arsenic | Mg/kg As | 0.3 max | <0.01 |
| Total Lead | Mg/kg Pb | 1 max | <0.1 |
| Total Cadmium | Mg/kg Cd | 0.2 max | <0.01 |
| Total Mercury | Mg/kg Hg | 0.05 max | <0.03 |
| Total Nickel | Mg/kg Ni | 0.75 max | <0.05 |
| Total Chromium | Mg/kg Cr | 0.75 max | <0.03 |
| Total Selenium | Mg/kg Se | 2.6 max | <0.2 |
| Total Antimony | Mg/kg Sb | 2.6 max | <0.2 |
| Total Bromide | Mg/kg Br | <50 | 32 |

Physical Characteristics

Typical Sieve Analysis					% through Sieve

3.35mm		99.7

1.7mm			56.1

0.6mm			1.8

Note that the specification for passing 0.6mm sieve is 10% maximum