Hydrosoft Tablets are premium quality compacted salt, one of a range of superior products for water softener regeneration.  The specification is assured by an audited Quality system to ISO 9001:2008, so ensuring consistent performance.

## CHEMICAL SPECIFICATION

Test methods used are BS998:1990 or equivalent, except appearance which is a visual assessment.

# Property			Unit			Specification			Typical

# Analysis

# Appearance						White

Assay (dry basis)		% m/m NaCl		 ≥99.9				99.9

Moisture			% m/m H20		≤0.05				0.03

Insoluble Matter		mg/kg			< 100				<10

*Alkalinity			mg/kg			< 150				80

Na2 CO3

# *Sulphate			mg/kg			< 500				216

Na2 SO4

Total Iron			mg/kg Fe		<3				0.2

*Total Calcium		mg/kg Ca		< 20				5.2

*Total Magnesium		mg/kg Mg		< 5				0.19

*Total Copper			mg/kg Cu		< 0.2				0.05

*Total Arsenic			mg/kg As		< 0.2				< 0.2

*Total Lead			mg/kg Pb		< 0.05				0.01

*Total Cadmium		mg/kg Cd		< 0.1				< 0.01

*Total Mercury		mg/kg Hg		< 0.05				<0.03

Anti-caking agent		mg/kg			None added			Not detected

*measured on PDV

## TYPICAL PHYSICAL CHARTERISTICS

Typical tablet weight			10g Approx

Typical tablet dimension		24 x 24 x13mm approx

Typical % m/m whole Tablets	>90

Typical % m/m Fines			<2