Product: Refined Sea Salt

Description

Refined salts are the product of a natural and environmentally friendly process utilizing the unique Dead Sea Waters. Production is mainly by a solar evaporation process, which takes advantage of the climatic conditions at the Dead Sea area. The final result is a natural, high purity product that can be tailor fitted to the customer’s requirements.

# Chemical Analysis				Typical %		Min / Max %

Sodium Chloride (NaCl)		 	99.8      		99.5 min.

Calcium (Ca++)              			0.05			0.08 max.

Magnesium (Mg++)         			0.02 			0.05 max

Insolubles 					0.03			0.03 max

Sulphate (SO4=)				0.12		 	0.25 max.

Moisture (H²O					0.1 			0.15 max

Potassium (K+)				0.1			0.25 max

Fe	10 ppm max

Cu	2.5 ppm max

Pb	1 ppm max

As	1 ppm max

Granulometry

Min 75% between 2 mm. to 5 mm.

Density 	1.11

Packaging

25kg Polyethylene bags

1200kg Polypropylene bags

Impurity Information

Due to the larger grain size of this material, there can be a higher volume of impurities such as small stones present compared to the finer material, therefore we market this material as technical grade as it may not be suitable for some food applications.

Fumigation

All the products manufactured and supplied by us, packaged and transported on wooden pallets, are treated according to ISPM 15 requirements. Our wooden pallets are marked by our pallets’ suppliers as authorised by PPIS.

Storage Conditions

If stored in a cool and dry place and with proper packaging, shelf-life should remain 2 years after production date.