Name, formula:		Sodium Chloride, NaCl

Table salt, common salt

Appearance: 			White with some grey/black by-minerals

CAS-No	: - 7647-14-5		EINECS-No: 231-598-3

Chemical analysis:				Typical		Methods

Sodium Chloride				99%			ASTM 534-08

Calcium & Magnesium			0.3%			ISO 2482

Sulphate					0.7%			ISO 2480

Granulometry				Typical		Methods

>4.0mm					15%			EN1235

1.25-4.00mm					78%

<1.25mm					7%

Bulk density:					1.050 - 1.250 kg/m3	EN1236

Forms of delivery:

Bags		In 25kg PE bags on pallet

8 layers of 5 bags = 1,000 kg

Pallet protection: shrink-wrapped

1000kg bags on pallets

Other delivery forms on request

*Please note this is a food Grade product, it also contains no anti-caking agent therefore may cake in storage.