Name, formula:		Sodium Chloride Brine

Trade name:			Brine

Quality:	Liquid, odourless

Ingredients:	*Sodium Chloride 20%  - H2O 80%

Typical Chemical Analysis

| Sodium Chloride NaCl | 99.5% (dry basis) |
| --- | --- |
| Calcium Sulphate Ca SO4 | 0.05% |
| Magnesium Sulphate Mg SO4 | 0.05% |
| Magnesium Chloride MgC1 | 0.01% |

*The dissolved solid content breaks down as above.

Chemical Composition

| Parameter | Units | Specification |
| --- | --- | --- |
| Sodium Chloride | % m/m | 20 min |
| Water Insolubles | mg/l | 50 max |
| Iron | mg/l | 0.1 max |
| Copper | mg/l | 0.01 max |
| Arsenic | mg/l | 0.2 max |
| Lead | mg/l | 0.05 max |

Bulk density:			1.05 - 1.25 g/cm3

According to DIN (ISO) 3944

Forms of delivery:

800ltr IBC

1000ltr IBC

4 x 5ltr Tubs

15ltr Jerry Can