Description/Appearance: 	White/ Dark Pink. Product is free from Additives

Odour/Taste:		 Odourless

Shelf Life/Storage:  	Store in a tightly closed container, in a cool dry and ventilated area. Protect against physical damage.

| Product Composition |
| --- |
| Ingredient Name | % of total | Country of origin |
| NaCl (on dry salt) | 97-98 min | Pakistan |
| MgSO4 | 0.50 max |  |
| Iron(Fe) | 10ppm max |
| Moisture | 0.2 max |
| Calcium (Ca) | 0.15 max |

Grain Size

3 ½ - 10 mesh (2 -5.66mm)

Packaging

Available in 25kg sized bags.