Industrial PDV Salt is a non-food grade of salt suitable for a wide range of industrial and chemical uses.  Low sulphate, bromide and moisture levels contribute to the high chemical purity which is required for most industrial applications.  This purity is assured by a quality system registered to ISO 9001 and a commitment to Total Quality Management. Occasionally trace amounts of harmless calcium carbonate scale, visible as tiny brown specs can be found in Industrial PDV salt.

Chemical Specification

Test methods used are BS 7319:1990 or equivalent, except appearance which is a visual assessment.

# Property			Unit			Specification		Typical

# Analysis

# Appearance						Predominantly

# White Crystalline

Assay (dry basis)			% m/m NaCl		≥ 99.9			> 99.9

Surface Moisture			% m/m H20		 ≤0.1			0.03

Insoluble Matter			mg/kg			< 50 			< 20

Alkalinity			mg/kg			< 150 			70

Na2 CO3

# Sulphate				mg/kg			< 500 			195

Na2 SO4

# Sodium (E535)			mg/kg			< 20			7

Hexacyanoferrate ll		Na4 Fe (CN)6

Total Iron			mg/kg Fe		< 5			2

Total Calcium			mg/kg Ca		< 20			5

Total Magnesium			mg/kg Mg		< 5 			1.5

Total Copper			mg/kg Cu		2 max			<0.1

Total Arsenic			mg/kg As		0.3 max			< 0.01

Total Lead			mg/kg Pb		1 max			<0.1

Total Cadmium			mg/kg Cd		0.2 max			<0.01

Total Mercury			mg/kg Hg		0.05 max		<0.03

Total Nickel			mg/kg Ni		0.75 max		<0.03

Total Chromium			mg/kg Cr		0.75 max 		<0.03

Total Selenium			mg/kg Se		2.6 max			<0.2

Total Antimony			mg/kg Sb		2.6 max			<0.2

Total Bromide			mg/kg Br		<150			80

## PHYSICAL CHARTERISTICS

Typical Pouring Density	1.25 – 1.30 g/ml

Typical Sieve Analysis		BS410 ref	% through Sieve

16 (1000µm)	100

22 (710µm)	99.9

30 (500µm)	97.1

52 (300 µm)	39.5

85 (180 µm)	9.0

Available in Bulk loads, 25kg or 1 metric tonne bags.