Name, formula:		Sodium Chloride and Peacock 563 Mix

Trade name:			Pro Coat

Quality:	Crystalline white high quality marine salt, clear syrupy liquid, odourless

Typical treat for all applications:	0.25 – 1.0% w/w

Sodium Chloride Specification

Typical chemical analysis:	NaCl					≥99.0%

Sulphate SO4				<0.5%

Insolubles				≤0.15%

H20 (loss of mass at 110c)

Typical screen analysis:	Above 6.3mm 				≤5%

Passing 6.3mm 			≥ 95%

Passing 3.26mm			40-60%

Passing 300 µm			≤5%

Moisture				≤4% (loss of weight at 110c)

Treated with Anti-caking treatment

Peacock 563 Specification

Description:   		Water based, cost effective multi-metal corrosion inhibitor,

which contains no secondary amines.

Typical Properties

Appearance	                             Clear straw coloured liquid

pH (5 % solution)		      7.4 – 7.9

Specific Gravity @ 15°C	      ca. 1.12

IP 287 Breakpoint		      100 : 1

Aluminium staining test	No stain or blemish

Additional Information: 	Remains a mobile liquid, even at low temperatures

Does not dry to form sticky or gummy residues

Nitrite & boron free

Excellent hard water compatibility

Low foaming tendency

Contains no solvents

All components are approved for incidental food contact

Forms of delivery:

Bags:

1000kg